Membrane:

BW-8040

| Model Number MR-BW-8040 |  |
| --- | --- |
| 400 (37) | Effective membrane area ft2 (m2) |
| 255 (1.55) | Operating Pressure psi (MPa) |
| 11000 (41) | Average yield GPD (m3/day) |
| 99.5 | Salt rejection (%) |
| 15 | Recovery Rate (%) |
| 600 (42) | Max. Operating Pressure psi (MPa) |
| 45 | Max. inflow temperature (C°) |
| 5 | Max. inflow SDI |
| 80 (18) | Max. water flow GPM (m3/hr) |
| < 0.1 | Free Chlorine concentration |
| 3-10 | Continuous running water PH range |
| 2-11 | Chemical cleaning water PH range |
| 15 (0.1) | Max. single membrane element pressure drop |

Sea Water Membrane 8040

| Model Number MR-SW-8040 |  |
| --- | --- |
| 400 (37) | Effective membrane area ft2 (m2) |
| 800 (5. 5) | Operating Pressure psi (MPa) |
| 6000 (22.7) | Average yield GPD (m3/day) |
| 99.75 | Salt rejection (%) |
| 93 | Boron-removing Rate (%) |
| 31 | Feed spacer (mil) |
| 25 | Test temperature (C°) |
| 75 (17) | Max. feed flow GPM (m3/hr) |
| < 0.1 | Free Chlorine concentration |
| 3-10 | Continuous running water PH range |
| 32800 | Test water concentration (ppm) |
| 7.5 | Test water PH |
| 15 (0.1) | Max. Pressure drop for each element psi (MPa) |